# GRADES AVAILABLE – HYUNDAI SERVO GEAR OIL

# CHARACTERISTICS

| Kinematic Viscosity, cSt @ 100(C | 13.5 - 17.0 |
| --- | --- |
| Viscosity Index, Min. | 100 |
| Flash Point, (COC)(C, Min. | 165 |
| Pour Point (C, Max. | (-) 27 |
| Copper Corrosion 121(C, 3 hrs., Max. | 1b |

# Text boxes

# PERFORMANCE BENEFITS

#	Enables smooth shifting of gears

#	Gives outstanding protection against rust and corrosion.

#	Provides improved seal life due to good compatibility with seal materials normally used in modern gear boxes.

#	Gives extra fuel economy and excellent all weather performance due to improved cold weather properties.

# PERFORMANCE STANDARDS

Hyundai Servo Gear Oil meet the following specifications :

*	API GL 4

*	IS 1118 - 92 EP Type GL4 SAE

80W-90

# MANUFACTURER’S APPROVAL

- M/s. Hyundai Motors India Ltd as Genuine Oil.

DESCRIPTION

Hyundai Servo Gear Oil is a premium quality automotive gear lubricant specially formulated to meet the requirements of Hyundai Vehicles.  The compactness of the new class of gearboxes with increased power density, low clearances and with gear assembly partly submerged in the oil, results in the gear oil being subjected to greater operational severity.  It is tailor-made for such applications with superior thermo-oxidative stability, high EP and antiwear properties, low copper activity, enhanced protection against corrosion, rust and formation of sticky deposits.

# APPLICATION

Hyundai Servo Gear Oil is specially recommended for Hyundai Vehicles.   This oil can be used in transmission systems of all models of Hyundai Vehicles.