# GRADES AVAILABLE – KINETIC ULTRA 2T OIL

# CHARACTERISTICS

|  | Kinetic Ultra 2T Oil |
| --- | --- |
| Kinematic Viscosity @ 40(C, cSt | 48-70 |
| Flash Point (COC), (C, Min | 70 |
| Sulphated Ash, % Wt., Max | 0.25 |

# Text boxes

# PERFORMANCE BENEFITS

- Low exhaust smoke

- Maintains engine cleanliness

- Minimises spark plug fouling

- Reduces port deposits and ring sticking

- Prevents seizure and scuffing

- Is easily pumpable by oil injection system

# PERFORMANCE STANDARDS

Meets

- JASO FC specifications.

# MANUFACTURERS APPROVAL

- M/s. Kinetic Motors Ltd., and Kinetic Engineering Ltd. have approved Kinetic Ultra 2T Oil for their two stroke scooters and mopeds respectively.

# APPLICATION

Kinetic Ultra 2T Oil is recommended for lubrication of Kinetic Pride, DX, ZX, Safari and Luna Mopeds.   The recommended dosage of Kinetic Ultra 2T Oil is 20 ml of oil per litre of petrol.

DESCRIPTION

Kinetic Ultra 2T Oil is low smoke semi- synthetic two stroke engine oil developed to meet the critical requirements of high performance two stroke engines manufactured by M/s. Kinetic Motors Ltd and Kinetic Engineering Ltd.  It is blended from selected base stocks and additives to minimise spark plug fouling and preignition, prevent rusting, minimise deposit formation and provide protection against seizure, scuffing and wear.  It contains a diluent for easy mixing with gasoline.