# GRADES AVAILABLE - SERVO GEAR HP 75W- 90

# CHARACTERISTICS

| SAE GRADE | 75W - 90 |
| --- | --- |
| Kinematic Viscosity cSt @ 100(C | 13.5-15.5 |
| Viscosity Index, Min. | 130 |
| Flash point (COC), (C Min. | 150 |
| Pour Point, (C Max. | (-) 39 |

# Text boxes

# PERFORMANCE STANDARDS

Servo Gear HP oils meets:

- API Service GL 4

- IS: 1118-1992

- UK Defence CS 3000A

- US military MIL-L-2105

# PERFORMANCE BENEFITS

Servo Gear HP oils

- Satisfy the lubrication requirements of a wide variety of gears.

- Provide protection against wear, due to good EP characteristics

- Give long service life even under high temperature operation since it has excellent oxidation stability

- Provide good protection against corrosion

DESCRIPTION

Servo Gear HP 75W-90 is hypoid gear oil having long service life due to their extremely good oxidation stability.   These oils are blended from selected base stocks and contain additives to provide extreme pressure, anti-rust-corrosion characteristics

# APPLICATION

Servo Gear HP 75W-90 is recommended for hypoid, spiral bevel or worm gear transmission systems of cars, buses and highway trucks requiring EP type lubricants.  This oil having very low pour point , can be used for power transmission unit of vehicles operating at sub zero temperature.