# GRADES AVAILABLE - SERVO PREMIUM (N) 15W-40

#### CHARACTERISTICS

| SAE GRADE | 15W-40 |
| --- | --- |
| Kinematic Viscosity, cSt @ 100(C | 13.5 – 15.5 |
| Viscosity Index, Min. | 130 |
| TBN, mg KOH/g | 9.5 – 11.5 |
| Flash Point, (COC)(C, Min. | 200 |
| Pour Point (C, Max. | (-) 24 |

# Text boxes

# PERFORMANCE BENEFITS

#	Reduced engine scuffing and bore polishing.

#   High engine cleanliness.

#   Maximum protection from wear and deposits.

#   Suitable for mixed fleet operation.

#   Improved control of oil consumption.

#   Easier cold starting.

# Excellent all weather performance due to improved cold weather properties.

#  Catalytic Converter compatible.

# PERFORMANCE STANDARDS

*	API CH-4

*	MB 228.3

*	ACEA E3-96

APPROVAL

*	M/s MTU, Germany for the oil category 2 for the application in MTU engines & DDC engines series 2000 & 4000.

DESCRIPTION

Servo Premium (N) 15W-40 is API certified, premium commercial multipurpose diesel engine oil. The oil is designed for the most severe performance requirements of new generation diesel engines for on and off highway operations. It assures outstanding protection against high temperature engine deposits, oil degradation, oil thickening and corrosion resistance. The oil is having excellent shear stability to maintain viscosity under severe, high temperature operations.

# APPLICATION

Servo Premium (N) 15W-40 is recommended for new generation commercial diesel vehicles of both American and European design such as Caterpillar and Cummins operating on Heavy duty              on-highway and off-highway equipments.