# GRADES AVAILABLE – SERVO SUPER PLUS 20W-40

# CHARACTERISTICS

| SAE GRADE | 20W- 40 |
| --- | --- |
| Kin. Vis. cSt @ 100(C | 13 .5 – 15 .5 |
| Viscosity Index, Min. | 110 |
| Flash point (COC), (C Min. | 200 |
| Pour Point, (C Max. | (-) 6 |
| TBN mg KOH/gm | 9.5–12.5 |

# Text boxes

# PERFORMANCE BENEFITS

Servo Super Plus oil

- Provide excellent resistance against wear and deposits in automotive supercharged diesel engines

- Have exceptional thermal and oxidation stability to resist decomposition in supercharged engines operating with high ring zone temperature.

- Provide absolute control of corrosive wear that may result from use of high sulphur fuels because of good built-in alkaline reserves.

- Maintain a high order of engine cleanliness

# PERFORMANCE STANDARDS

Servo Super Plus oil meets the following specifications:

- US MIL-L 2104C

- API CF/CD

- E-DL 3 of IS:13656-2002

- Caterpillar Series 3

- MACK T-7 test for oil thickening tendency.

- Sequence III F

.

DESCRIPTION

Servo Super Plus 20W 40 is a heavy duty diesel engine oil.  This oil is blended from selected highly refined, high viscosity index base stocks and contain well balanced group of additives, to provide high detergency, dispersancy and anti oxidation characteristics to meet the stated performance standards.

# APPLICATION

Servo Super Plus 20W 40 is recommended for

naturally aspirated, highly supercharged and turbocharged diesel engines  operating under severe duty conditions in all seasons .