# GRADES AVAILABLE – SERVO ULTRA KB 10W, 30

# CHARACTERISTICS

| SAE GRADE | 10W | 30 |
| --- | --- | --- |
| Kinematic Viscosity cSt @ 100(C | 5Min. | 10 – 12 |
| Viscosity Index, Min. | 95 | 90 |
| Flash point (COC), (C Min. | 200 | 220 |
| Pour Point, (C Max. | (-) 27 | (-) 9 |
| TBN mg KOH/gm | 9.5 – 11.5 | 9.5 – 11.5 |

# Text boxes

# PERFORMANCE STANDARDS

Servo Ultra KB oils meet the following specifications:

- API CD

- US MIL-L-45199B

- Caterpillar Series 3

- Meets BEML ED 10CD for KB 10 & BEML ED 30 CD for KB 30.    E-DL 2 of IS:13656-2002 specifications

MANUFACTURERS APPROVAL

Servo Ultra KB oils are approved by the leading manufactures including

- Bharat Earth Movers Ltd., Bangalore

# PERFORMANCE BENEFITS

- Effectively combat the deleterious products of combustion associated with high sulphur fuels, thus minimising deposits and wear.

- Maintain excellent engine cleanliness.

- Minimise deposits resulting from high output, low speed, low temperature operations.

- Provide excellent control of cold sludge and corrosive wear.

- Possess excellent oxidation stability ensuring long service life especially in transmission systems.

DESCRIPTION

Servo Ultra KB oils are heavy duty diesel engine oils, and are blended from highly refined, high viscosity index base stocks and contain appropriate dosages of detergent-dispersant and antioxidant additives to meet the stated performance standards.

# APPLICATION

Servo Ultra KB oils are recommended for all classes of supercharged diesel engines of high speed, high output such as those in Earth moving / Off-highway equipment. It is also effective used in Transmission systems of Caterpillar equipment.