# GRADES AVAILABLE – SERVO ULTRA 10W, 20, 30, 40, 50

# CHARACTERISTICS

| SAE GRADE | 10W | 20 | 30 | 40 | 50 |
| --- | --- | --- | --- | --- | --- |
| Kinematic Viscosity cSt @ 100(C | 5Min. | 6 – 8 | 10 – 12 | 13 – 15 | 18 – 20 |
| Viscosity Index, Min. | 100 | 95 | 95 | 90 | 90 |
| Flash point (COC), (C Min. | 200 | 200 | 220 | 225 | 230 |
| Pour Point, (C Max. | (-) 27 | (-) 6 | (-) 6 | (-) 6 | (-) 6 |
| TBN mg KOH/gm | 9.5 – 11.5 | 9.5 – 11.5 | 9.5 – 11.5 | 9.5 – 11.5 | 9.5 – 11.5 |

# Text boxes

# PERFORMANCE STANDARDS

Servo Ultra oils meet the following specifications:

- API CD

- US MIL-L-45199B

- Caterpillar Series 3

- E-DL 2 of IS:13656-2002 specifications

Servo Ultra oils are approved by the leading manufactures including

- Bharat Earth Movers Ltd ., Bangalore

- Escorts Ltd., Faridabad

# PERFORMANCE BENEFITS

Servo Ultra oils

- Effectively combat the deleterious products of combustion associated with high sulphur fuels, thus minimising deposits and wear.

- Maintain excellent engine cleanliness.

- Minimise deposits resulting from high output, low speed, low temperature operations.

- Provide excellent control of cold sludge and corrosive wear.

- Possess excellent oxidation stability ensuring long service life especially in transmission systems.

DESCRIPTION

Servo Ultra oils are heavy duty diesel engine oils, and are blended from highly refined, high viscosity index base stocks and contain appropriate dosages of detergent-dispersant and antioxidant additives to meet the stated performance standards.

# APPLICATION

Servo Ultra oils are recommended for all classes of supercharged diesel engines of high speed, high output such as those in:

- Heavy duty diesel vehicles / Tractors

- Earth moving / Off-highway equipment

- Transmission systems of Caterpillar equipment

- Large generating sets

Servo Ultra 10 meets the requirements of hydraulic fluid Type C2 specification of Detroit Diesel Allison, Division of General Motors Corporation, USA.