GRADES AVAILABLE – SERVO FORCE GREASE

# CHARACTERISTICS

| GRADE | Servo Force Grease |
| --- | --- |
| NLGI No. | 3 |
| Colour | Brown |
| Structure | Smooth |
| Soap Type | Lithium |
| Worked Penetration @ 25(C, (60 Strokes) | 220-250 |
| Drop Point, (C, Min. | 180 |

# Text boxes

# PERFORMANCE BENEFITS

- Excellent resistance to water washout

- Superior oxidation and structural stability

- High degree of antirust and anticorrosion properties.

- Give outstanding performance under varying operating conditions.

- Suitable for lubrication under sub-zero (-25(C) to reasonably high (140(C) temperature conditions.

# PERFORMANCE STANDARDS

Meets specification of Association of American Railroads (AAR-M-942-81) with deviation in consistency and passes SKF Emcor corrosion test and WD-17-MISE-92 specifications.

APPROVAL:

Servo Force Grease is approved by M/s. Force Motors Ltd as Genuine Grease for use in the vehicles manufactured by them.

# APPLICATION

This grease is specially developed for the lubrication of antifriction bearings of Force Motors  Vehicles to give longer service life.

The grease has been evaluated for wheel bearing applications for automotive purposes.

DESCRIPTION

Servo Force Grease is developed for wheel bearing lubrication of all Force Motors vehicles. It is a premium quality, lithium soap, multipurpose grease.    The grease is manufactured from high viscosity index base oils and select additives with superior performance benefits.