# GRADES AVAILABLE - SERVO GEAR SUPER ALT 85W-140

# CHARACTERISTICS

| SAE GRADE | ALT 85W-140 |
| --- | --- |
| Kinematic Viscosity cSt @ 100(C | 28 – 32 |
| Viscosity Index, Min. | 90 |
| Flash point (COC), (C Min. | 180 |
| Pour Point, (C Max. | (-) 18 |

# Text boxes

# PERFORMANCE STANDARDS

Servo Gear Super ALT 85W-140 meets

- API Service GL 5

- US military MIL-L-2105D

#### APPROVAL

- Ashok Leyland Ltd., Chennai for every 48000 KMs.

# PERFORMANCE BENEFITS

- Provide protection against wear, due to good EP characteristics

- Give long service life even under high temperature operation since it has excellent oxidation stability.

- Provide good protection against corrosion.

- Keep the differentials clean and free of deposits.

DESCRIPTION

Servo Gear Super ALT 85W-140 oil is an extreme pressure automotive gear lubricant. This oil is blended from selected base stocks and contain specific additive package to provide extreme pressure, anti-rust-corrosion characteristics.  This formulation is specially  developed for hypoid type rear axles of Ashok Leyalnd vehicles.

# APPLICATION

Servo Gear Super ALT 85W-140 oil is  recommended for hypoid type of rear axle  of Ashok Leyland vehicles.