# GRADES AVAILABLE - SERVO PREMIUM ALT 15W-40

#### CHARACTERISTICS

| SAE GRADE | ALT 15W-40 |
| --- | --- |
| Kinematic Viscosity, cSt @ 100(C | 14.0 – 15.0 |
| Viscosity Index, Min. | 135 |
| TBN, mg KOH/g | 8.5 – 11.5 |
| Flash Point, (COC)(C, Min. | 200 |
| Pour Point (C, Max. | (-) 24 |

# Text boxes

# PERFORMANCE BENEFITS

#	Reduced engine scuffing and bore polishing.

#    High engine cleanliness.

#    Maximum protection from wear and deposits.

#    Suitable for mixed fleet operation.

#    Improved control of oil consumption.

#    Easier cold starting.

# Excellent all weather performance due to improved cold weather properties.

# PERFORMANCE STANDARDS

*	API CF4

*	MB 228.1

Servo Premium ALT 15W-40 is approved by:

*          Ashok Leyland Ltd, Chennai.

DESCRIPTION

Servo Premium ALT 15W-40 is a premium quality  commercial  diesel engine oil. The oil is designed for the most severe performance requirements of modern, highly rated turbo charged diesel engines in the over the road transport fleet applications and also off highway operations. It assures outstanding protection against high temperature engine deposits, oil degradation, oil thickening and corrosion resistance. The oil is having excellent shear stability to maintain viscosity under severe, high temperature operations.

# APPLICATION

Servo Premium ALT 15W-40 is recommended for  Ashok Leyland commercial  vehicles  complying with Bharat Stage-I Emission Norms. It is also suitable for earlier models.